## Slide 1: POLARBEAR-2 Cryogenic Half-Wave Plate
Charlie Hill (Grad Student, UC Berkeley)
w/ Akito Kusaka, Adrian Lee, and Paul Barton (LBNL)
B-modes in Space
2017-12-05

## Slide 2: POLARBEAR-2 optical system
Off-axis Gregorian telescope
95/150 GHz dichroic detectors
Three alumina reimaging lenses
365-mm-diameter focal plane
4 deg field of view
PB2 camera
Secondary
CMB Photon
190 cm
5 m

## Slide 3: Motivation for a cryogenic half-wave plate
A cryogenic HWP (CHWP) improves PB2 mapping speed by ~2x compared to a warm HWP
Impact of HWP temp on MS
Warm HWP for PB2a
An ambient-temperature half-wave plate (HWP) has been constructed for PB2a
500 mm

## Slide 4: PB2 CHWP optical stack
Stack Element | Thickness [mm] | Index of Refraction | Loss Tangent [10-4]
Top AR Layer: SiO2 TS | 0.435 ± 0.025 | 1.39 | < 10
Bottom AR Layer: Al2O3 TS | 0.265 ± 0.025 | 2.30 | < 10
Sapphire Ordinary Axis | 3.90 ± 0.2 | 3.37 | < 0.5
Sapphire Extraordinary Axis |  | 3.05 | 
D = 510 mm sapphire
Parameter | Value
A-plane | ± 1 deg
Parallelism | < 0.050 mm
Bow | < 0.010 mm
2-layer thermal spray AR
Band | Refl | Abs
95 GHz | 0.5 % | < 1.4 %
150 GHz | 0.6 % | < 0.8 %
Achromatic 3-stack HWP
Band | Mod Eff
95 GHz | 98.9 %
150 GHz | 99.1 %
95 GHz
150 GHz

## Slide 5: PB2 CHWP rotation mechanism
Magnetic levitation bearing
Magnetic motor
NdFeB Rotor
YBCO Stator
Solenoids
Flux pinning concept
Motor operation concept
~100 N/mm spring constant at 5 mm separation and 77 K
< 10 mW dissipation at 2 Hz and 77 K
Three-phase operation
< 100 mW motor power dissipation during 2 Hz continuous rotation
600 mm
470 mm

## Slide 6: PB2 CHWP encoding and driving
Motor (and angle) encoding done using photodiode-LED pairs and a slotted plate
  IR LED emitters (SPIDER)
  Silicon photodiodes (SPIDER)
  Quadrature readout
  1 reference pulse per cycle (for absolute angle)
  0.3 deg angular resolution (540 slits in slotted plate)
  < 1 us timestamp jitter (leading to 10 uRad angle jitter using interpolation)
  PD amplified warm and signal fed to dual Half-H drivers to excite coils

## Slide 7: Table-top motor test

## Slide 8: Motor performance
Table-top testing results
  1/f knee at < 1 mHz  very stable rotation
  Measured frictional dissipation < 50 mW
  No pathologies in power spectrum indicates functional DAQ

## Slide 9: PB2 CHWP gripper
“Grip” to align the HWP
“Ungrip” to spin the HWP
Three gripper modules to constrain HWP position
Conceptual cartoon
Gripper module
Vacuum feedthrough actuator
G10 isolation
50 K Frelon bearing
Copper contact finger with slip-ring contact for stationary thermometry
Bearing
Feedthrough actuator
Therm iso
Coupling finger
CF flange
Red = 300 K
Blue = 50 K
Slipring contact
Gravity

## Slide 10: PB2 CHWP implementation

## Slide 11: PB2 CHWP implementation
CHWP system currently under evaluation at LBNL

## Slide 12: PB2 vs LiteBIRD CHWP
PB2 | LiteBIRD
Gripper: Linear Actuator | 
300 K (ATM ambient) | 4 K (L2 ambient)
1e3 Torr (ATM ambient) | 1e-10 Torr (L2 ambient)
~3 mm throw (bearing sag at 100 K) | ~2 mm throw (bearing sag at 4 K)
50 lb holding force (HWP weight) | > 250 lbs (15g launch RMS, 4~5σ peak force)
Gripper: Compactness | 
~12” gripper footprint in radius | ~< 6” gripper footprint in radius
Gripper: Robustness | 
~10 gripper motions during operation | Many gripper motions possibly needed for periodic cooling
HWP Cooling | 
Strapped alumina filter on both sides of the HWP for good radiative cooling | Exposed to environment beyond entry aperture, no controlled radiative coupling
Bandwidth | 
2:1 (2 bands, 75 – 165 GHz) | 8:1 (12 bands, 35 – 270 GHz)

## Slide 13: Backup Slides

## Slide 14: Integrated rotor/stator assembly

## Slide 15: PB2a WHWP

## Slide 16: Slip-ring thermometer
Prototype
  Measured the temperature of stationary rotor
  Acted as a switch for the “gripped” mode
  Designed to lightly touch while rotating
Full-scale
  Only designed to measure stationary
  Will rely on remote thermometry for floating measurement
Slip-ring contact
Slip-ring traces
Prototype system
Full-scale system
Slip-ring contact
Slip-ring traces